MECH 4310 Analysis of Composite and Multifunctional Materials

HOMEWORK #3

Due February 14, 2019

1.  Given the following material,

E11=100GPa, E22=18GPA, n12=0.33, G12=10GPa.

- Determine the Q, and S matrices.

- Determine the strains if the stresses are given as (assume the fibres are aligned with the x-direction):

xx = 100 MPa			yy = -30 MPa			xy = 60 MPa.

- Find the Qbar and Sbar matrices if the material angle (the 11 direction) is 30 degrees from the x-direction.

- Determine the strains for the stresses in b) for the angle in c).

- Plot the effective properties as a function of angle and comment on the results

2. Check out the site:

https://netcomposites.com/guide-tools/guide/manufacturing/

- Review the different types of composite fabrication techniques and identify which method might be more suitable for each of the following and explain why.

  - Sailboat hull

  - Fishing rod

  - Snowboard

  - Propane tank

  - Bicycle wheel

- List and explain the role of the materials used in the vacuum bagging process

- What are the key differences between the wet lay-up and prepreg composite manufacturing techniques and what are the primary concerns when selecting either approach.