MECH 4310 Analysis of Composite and Multifunctional Materials

HOMEWORK #4

Due Thursday March 21st at 10:00

Given the material with

E11=170GPa, E22=10GPA, n12=0.3, G12=13GPa.

with the following layups. Assume that each ply has a thickness of 0.2mm and you may use the excel code posted on the website (assignment page)

- [0/-45/45/90]s

- [0/15/30/45/60/75/90]

- Evaluate the ABD matrices and comment on the results

- Determine the effective extensional and flexural properties

- Plot the stresses and Strains in terms of both the global and material coordinates for the following loading scenarios

- Nxx=100N/m

- Mxx=100Nm/m

- T=-125oC

- Determine the stress resultant Nx and the moment resultant Mx individually that would cause the first ply to fail for both the max stress and Tsai-Hill failure criteria. Use the material limit data for graphite epoxy provided in the text (data provided in spreadsheet)

- Determine the stress resultant Nx and the moment resultant Mx individually that would cause the first ply to fail for both the max stress and Tsai-Hill failure criteria if in addition the composite is subject to T=-125oC.